### Immunomodulatory Effects of Carbonate Hydroxyapatite and Ellagic Acid-Modified Calcium Hydroxide During Pulp Healing in a Rat Pulp Perforation Model

Catur Septommy1,2) Intan Nirwana3), Ira Widjiastuti4)

1) Doctoral Study Program, Faculty of Dental Medicine, Universitas Airlangga, Surabaya, Indonesia.

2) Department of Biomaterial, Faculty of Dental Medicine, Institut Ilmu Kesehatan Bhakti Wiyata, Kediri, Indonesia

3) Dental Materials Division, Department of Basic Dental Science and Public Health, Faculty of Dental Medicine, Universitas Airlangga, Surabaya, Indonesia

4) Department of Conservative Dentistry, Faculty of Dental Medicine, Universitas Airlangga, Surabaya, Indonesia.

# Abstract

Background: Effective pulp healing depends on removing harmful stimuli and regulating inflammation. Carbonate hydroxyapatite (CHA) and ellagic acid (EA) possess bioactive and anti-inflammatory properties that may improve the performance of calcium hydroxide in vital pulp therapy. Objective: This study assessed the immunomodulatory effects of calcium hydroxide (CH) modified with carbonate hydroxyapatite and ellagic acid on macrophage accumulation, TNF-α, and IL-10 expression during pulp healing after perforation. Methods: Sixty male Wistar rats were divided into four groups: negative control (NC), calcium hydroxide (CH), calcium hydroxide with carbonate hydroxyapatite (CH-CHA), and calcium hydroxide with both carbonate hydroxyapatite and ellagic acid (CH-CHA-EA). Animals were sacrificed on days 3, 7, and 14. Macrophage counts were determined by hematoxylin and eosin staining, while TNF-α and IL-10 expression were measured immunohistochemically. Data were analyzed using one-way ANOVA and Tukey’s post hoc test (p<0.05). Results: On day 14, (CH-CHA-EA) showed the highest macrophage count (11.0±1.58) compared to NC (3.6±1.10; p<0.05). TNF-α expression was similar among groups on day 3 but lowest in (CH-CHA-EA) on day 14 (2.2±0.84) versus NC (12.0±1.87; p<0.05). IL-10 expression remained highest in (CH-CHA-EA) throughout, reaching 11.2±1.92 on day 14 compared to 6.2±1.92 in NC (p<0.05). Conclusion: Calcium hydroxide modified with carbonate hydroxyapatite and ellagic acid increased macrophage accumulation, elevated IL-10 expression, and reduced TNF-α expression during pulp healing. These results suggest the modified formulation has immunomodulatory effects that may support inflammation resolution and promote pulp repair and regeneration.

# INTRODUCTION

Preserving pulp vitality is a key goal in modern vital pulp therapy (VPT). After injury, dental pulp triggers a biological response involving inflammation, immune regulation, and repair to restore tissue balance. Recent studies indicate that controlled inflammation is essential for effective pulp healing and dentin repair. The shift from inflammation to repair depends on interactions among cytokines, immune cells, and dental pulp stem cells. Consequently, developing bioactive pulp-capping materials that regulate inflammation and support regeneration is now a major focus in regenerative endodontics.(1)

Pulp exposure from deep caries, trauma, or dental procedures triggers inflammation that helps remove harmful stimuli and supports pulp defense. However, excessive or persistent inflammation can disrupt tissue homeostasis, impair regeneration, and increase the risk of irreversible damage. Persistent inflammation may lead to pulpal necrosis and loss of vitality. Therefore, effective vital pulp therapy must protect exposed pulp tissue and properly manage inflammation to promote repair and regeneration.(2)

Macrophages play a central role in pulp healing by coordinating inflammatory and reparative responses after tissue injury. Initially, pro-inflammatory M1 macrophages support host defense by releasing mediators such as tumor necrosis factor-alpha (TNF-α). As healing progresses, macrophages transition to the M2 phenotype, which secretes anti-inflammatory cytokines like interleukin-10 (IL-10) and promotes tissue repair. This shift from a pro-inflammatory to a reparative phenotype is essential for resolving inflammation and enabling effective pulp healing and regeneration.(3)

Calcium hydroxide has long served as a reference material in vital pulp therapy due to its antibacterial properties, alkaline pH, and capacity to induce mineralized tissue formation. It releases hydroxyl and calcium ions, creating conditions that inhibit bacterial growth and promote reparative dentin formation after pulp injury. However, it has notable limitations, including high solubility, low mechanical strength, and vulnerability to microleakage. While calcium hydroxide can stimulate hard tissue bridge formation, the resulting reparative tissue often exhibits structural irregularities and less favorable histological features than newer bioactive materials.(4,5) These findings indicate that, although calcium hydroxide induces mineralization, its ability to modulate the inflammatory microenvironment and support optimal tissue regeneration is limited.

These limitations have prompted the search for alternative bioactive materials that support mineralization and modulate the inflammatory microenvironment. Carbonate hydroxyapatite (CHA) has recently gained attention as a bioactive biomaterial due to its close resemblance to the mineral phase of natural hard tissues. Carbonate substitution increases its similarity to biological apatite, enhancing resorbability and osteoconductive properties. Studies show that CHA supports cell attachment, proliferation, differentiation, and mineralized tissue formation, making it a promising candidate for regenerative applications. Its bioactivity and ion-release properties may also help create an environment more favorable for tissue repair and regeneration after injury.(6,7)

Ellagic acid (EA) is a polyphenolic compound found in pomegranate and other fruits, recognized for its strong anti-inflammatory and antioxidant effects. Studies show that EA reduces inflammatory responses by modulating cytokine-related signaling pathways, especially the NF-κB pathway. As a result, EA suppresses pro-inflammatory mediators and supports tissue repair. Incorporating EA into calcium hydroxide-based pulp-capping materials also decreases inflammatory cell infiltration and TNF-α expression, indicating an immunomodulatory effect that may resolve inflammation and enhance pulp healing.(8,9)

While calcium hydroxide, carbonate apatite, and ellagic acid each support tissue healing, their combined immunomodulatory effects on pulp repair are not well understood. Most research has focused on their antibacterial, mineralization, or regenerative properties (6,10), with limited study of their impact on the inflammatory microenvironment during pulp healing.(8) The effects of a combined Ca(OH)₂–CHA–EA formulation on macrophage responses and key inflammatory mediators, such as TNF-α and IL-10, remain unclear. Further research is needed to determine whether this biomaterial combination can modulate immune responses and support pulp repair.

This study evaluated a carbonate hydroxyapatite and ellagic acid-modified calcium hydroxide formulation as a potential immunomodulatory pulp-capping material in a rat pulp perforation model to address this knowledge gap. While previous research has focused on the antibacterial and mineralization-inducing properties of pulp-capping agents, the role of immune regulation in pulp healing is less understood. By assessing macrophage expression and cytokine levels of TNF-α and IL-10, this study aimed to clarify the immunological mechanisms underlying pulp repair.

# METHODS

Study Design

This laboratory study employed a post-test-only control-group design to assess the immunomodulatory effects of carbonate apatite- and ellagic acid-modified calcium hydroxide on pulp healing. Sixty healthy male Wistar rats (Rattus norvegicus) were randomly assigned to four groups: negative control (NC), calcium hydroxide (CH), calcium hydroxide with carbonate hydroxyapatite (CH-CHA), and calcium hydroxide with carbonate hydroxyapatite and ellagic acid (CH-CHA-EA). Each group included 5 animals per observation period (3, 7, and 14 days), for a total of 60 animals. Macrophage, TNF-α, and IL-10 expression were measured during healing following pulp perforation.

Experimental Animals

Healthy male Wistar rats (Rattus norvegicus), aged 20–28 weeks and weighing 270–320 g, were used. Animals were housed under standard laboratory conditions, with free access to food and water, and were acclimatized before the experiment. Health status was confirmed prior to inclusion. The experimental protocol was approved by the Health Research Ethical Clearance Commission, Faculty of Dental Medicine, Universitas Airlangga, Indonesia (Ethical Clearance No. 0109/HRECC.FODM/I/2026). All animal procedures followed institutional care and use guidelines.

Preparation of Pulp-Capping Materials

Calcium hydroxide [Ca(OH)₂] powder (Merck, Germany) served as the base pulp-capping material. Carbonate hydroxyapatite (CHA) powder was prepared as previously described using Indonesian limestone-derived hydroxyapatite and dry mechano-milling techniques and was used in this study.(11) For (CH-CHA), Ca(OH)₂ and CHA powders were mixed at a 1:1 (w/w) ratio. Ellagic acid (EA; 90% purity, Xi’an Biof Bio-Technology Co., Ltd., China) was prepared as a 12.5% solution by dissolving EA powder in 90% distilled water and 10% polyethylene glycol 400 (PEG 400) to a final volume of 100 mL. For (CH-CHA-EA), the Ca(OH)₂ and CHA mixture was combined with the EA solution at a 1:1 powder-to-liquid ratio before application.

Pulp Perforation Procedure and Material Application

Animals were anesthetized via intramuscular injection of 10% ketamine hydrochloride and 2% xylazine at 0.1 mL per 100 g body weight. After anesthesia, a cavity was prepared on the occlusal surface of the maxillary first molar using a low-speed handpiece with a 0.8-mm round bur. Pulp perforation was performed by gently probing the cavity floor with a dental explorer until bleeding and loss of resistance confirmed pulp exposure. Hemostasis was achieved with sterile paper points, and the exposed pulp was treated according to the assigned group. The cavity was sealed with conventional glass ionomer cement (GC Fuji, GC Corporation, Tokyo, Japan) to prevent bacterial contamination and maintain material retention during the observation period.

Histological and Immunohistochemical Analysis

At 3, 7, and 14 days post-treatment, animals were euthanized with an overdose of ketamine and xylazine at three times the anesthetic dose. The left maxillary jaw containing the first molar was immediately harvested and immersed in 10% neutral buffered formalin for 18 to 24 hours at room temperature until the pH reached approximately 7.0. Specimens were then decalcified in 10% EDTA solution at room temperature for 21 to 30 days, with daily solution changes until adequate tissue softening was achieved.

After routine tissue processing and paraffin embedding, serial sections were prepared for histological and immunohistochemical analysis. Macrophages were identified using hematoxylin and eosin (H&E) staining (HistoCore SPECTRA H&E Stains, Leica Biosystems). Immunohistochemical staining followed the manufacturer’s instructions, using anti-TNF-α antibody (Santa Cruz Biotechnology, Cat. No. sc-52746) and anti-IL-10 antibody (Santa Cruz Biotechnology, Cat. No. sc-8438).

Quantification of Macrophage, TNF-α, and IL-10 Expression

Microscopic evaluation was conducted at 1000× magnification. To reduce observational bias, approximately 20 fields were examined per specimen. Macrophage counts and TNF-α and IL-10 expression were assessed using light microscopy. All histological and immunohistochemical evaluations were performed in a blinded manner, with the observer unaware of the treatment groups.

Statistical Analysis

Statistical analyses were conducted using IBM SPSS Statistics version 25.0 (IBM Corp., Armonk, NY, USA). Data normality and homogeneity were evaluated with the Kolmogorov–Smirnov and Levene’s tests. Differences among groups were analyzed using one-way ANOVA, followed by Tukey’s HSD post hoc test. Statistical significance was defined as p < 0.05.

# RESULTS

Macrophage Expression During Pulp Healing

Macrophage expression increased over time, with the highest levels consistently in the Ca(OH)₂+CHA+EA group (CH-CHA-EA) (Table 1). On day 3, mean macrophage counts were 2.2±0.84 (NC), 4.8±1.30 (CH), 6.6±1.30 (CH-CHA), and 7.8±0.84 (CH-CHA-EA). One-way ANOVA indicated significant differences among groups (p<0.0001).

On day 7, macrophage expression increased further, with mean values of 2.8±0.84 (NC), 7.0±1.58 (CH), 8.0±1.58 (CH-CHA), and 9.4±1.52 (CH-CHA-EA) (Table 1). One-way ANOVA showed significant group differences (p<0.0001). Tukey’s post hoc analysis found all treatment groups had significantly higher macrophage expression than NC, with no significant differences among CH, (CH-CHA), and (CH-CHA-EA).

On day 14, macrophage counts rose to 3.6±1.10 (NC), 7.6±1.10 (CH), 9.2±1.79 (CH-CHA), and 11.0±1.58 (CH-CHA-EA). One-way ANOVA confirmed significant group differences (p<0.0001). (CH-CHA-EA) had significantly higher macrophage expression than NC and CH, but not (CH-CHA).

Table 1. Macrophage Expression During Pulp Healing Following Application of Different Pulp-Capping Materials

| Group | day 3 |  | day 7 |  | day 14 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | mean | SD | mean | SD | mean | SD |
| NC | 2,2 | 0,84 | 2,80 | 0,84 | 3,60 | 1,10 |
| CH | 4,8 | 1,3 | 7,00 | 1,6 | 7,60 | 1,10 |
| CH-CHA | 6,6 | 1,3 | 8,00 | 1,6 | 9,20 | 1,80 |
| CH-CHA-EA | 7,8 | 0,84 | 9,40 | 1,5 | 11,00 | 1,60 |

TNF-α Expression During Pulp Healing

TNF-α expression varied over time among groups (Table 2). On day 3, mean TNF-α expression ranged from 4.0±1.58 to 5.8±0.84, with no significant group differences (ANOVA, p=0.2434), indicating a similar early inflammatory response after pulp perforation.

By day 7, significant differences in TNF-α expression emerged (p<0.0001). (CH-CHA-EA) had the lowest expression (2.0±1.00), while NC, CH, and (CH-CHA) had higher values of 7.2±1.48, 7.8±1.30, and 6.6±1.14, respectively. Post hoc analysis confirmed significantly lower TNF-α expression in (CH-CHA-EA) compared to all other groups.

On day 14, TNF-α expression increased markedly in the negative control group (12.0±1.87), but remained low in CH (4.6±1.14), (CH-CHA) (4.8±1.30), and (CH-CHA-EA) (2.2±0.84). ANOVA showed significant group differences (p<0.0001), and Tukey’s test confirmed all treatment groups had significantly lower TNF-α expression than NC. (CH-CHA-EA) also had significantly lower expression than (CH-CHA).

Table 2. TNF-α Expression During Pulp Healing Following Application of Different Pulp-Capping Materials

| Group | day 3 |  | day 7 |  | day 14 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | mean | SD | mean | SD | mean | SD |
| NC | 5,6 | 2,1 | 7,20 | 1,50 | 12 | 1,90 |
| CH | 5,8 | 0,84 | 7,80 | 1,30 | 4,6 | 1,10 |
| CH-CHA | 5,0 | 1,0 | 6,60 | 1,10 | 4,8 | 1,30 |
| CH-CHA-EA | 4,0 | 1,6 | 2,00 | 1,00 | 2,20 | ,84 |

IL-10 Expression During Pulp Healing

IL-10 expression increased throughout the healing period, with the highest levels in (CH-CHA-EA) (Table 3). On day 3, mean IL-10 expression was 3.2±0.84 (NC), 5.2±1.30 (CH), 6.2±1.30 (CH-CHA), and 8.4±1.14 (CH-CHA-EA). Significant group differences were found (ANOVA, p<0.0001), with (CH-CHA-EA) showing the highest expression.

On day 7, IL-10 expression increased to 4.4±1.14 (NC), 7.4±1.82 (CH), 7.8±1.30 ((CH-CHA)), and 9.6±1.52 (CH-CHA-EA). Significant group differences were detected (p=0.0004), with (CH-CHA-EA) remaining significantly higher than NC, CH, and (CH-CHA).

On day 14, (CH-CHA-EA) maintained the highest IL-10 expression (11.2±1.92), followed by (CH-CHA) (9.2±1.30), CH (7.8±1.48), and NC (6.2±1.92). ANOVA showed significant group differences (p=0.0018), and post hoc analysis confirmed significantly higher IL-10 expression in (CH-CHA-EA) compared to NC and CH.

Table 3. IL-10 Expression During Pulp Healing Following Application of Different Pulp-Capping Materials

| Group | day 3 |  | day 7 |  | day 14 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | mean | SD | mean | SD | mean | SD |
| NC | 3,20 | 0,84 | 4,40 | 1,10 | 6,20 | 1,90 |
| CH | 5,20 | 1,30 | 7,40 | 1,80 | 7,80 | 1,50 |
| CH-CHA | 6,20 | 1,30 | 7,80 | 1,30 | 9,20 | 1,30 |
| CH-CHA-EA | 8,40 | 1,10 | 9,60 | 1,50 | 11,20 | 1,90 |

Figure 1. Effects of Carbonated Hydroxyapatite and Ellagic Acid-Modified Calcium Hydroxide on Macrophage, TNF-α, and IL-10 Expression During Pulp Healing

(A) Macrophage expression, (B) TNF-α expression, and (C) IL-10 expression on days 3, 7, and 14 after pulp perforation. Data are presented as mean ± SD (n = 5). Statistical significance was determined using one-way ANOVA followed by Tukey's HSD test. ns, not significant; *p < 0.05; **p < 0.01; ***p < 0.001; ****p < 0.0001.

| Picture Group NC(K1), CH (K2), CH-CHA (K3), CH-CH-EA (K4) | Picture Group NC(K1), CH (K2), CH-CHA (K3), CH-CH-EA (K4) | Picture Group NC(K1), CH (K2), CH-CHA (K3), CH-CH-EA (K4) |
| --- | --- | --- |
| day 3 | Day 7 | Day 14 |

Figure 2. Representative hematoxylin and eosin (H&E)-stained sections of perforated pulp tissue from the NC, CH, CH-CHA, and CH-CHA-EA groups. Arrows indicate macrophage infiltration within the pulp tissue. Original magnification ×1000.

| Picture Group NC(K1), CH (K2), CH-CHA (K3), CH-CH-EA (K4) | Picture Group NC(K1), CH (K2), CH-CHA (K3), CH-CH-EA (K4) | Picture Group NC(K1), CH (K2), CH-CHA (K3), CH-CH-EA (K4) |
| --- | --- | --- |
| day 3 | Day 7 | Day 14 |

Figure 3. Representative immunohistochemical staining showing TNF-α-positive cells in perforated pulp tissue following treatment with different pulp-capping materials. Brown staining indicates TNF-α immunoreactivity. Arrows indicate positively stained cells. Original magnification ×1000.

| Picture Group NC(K1), CH (K2), CH-CHA (K3), CH-CH-EA (K4) | Picture Group NC(K1), CH (K2), CH-CHA (K3), CH-CH-EA (K4) | Picture Group NC(K1), CH (K2), CH-CHA (K3), CH-CH-EA (K4) |
| --- | --- | --- |
| day 3 | Day 7 | Day 14 |

Figure 4. Representative immunohistochemical staining showing IL-10-positive cells in perforated pulp tissue following treatment with different pulp-capping materials. Brown staining indicates IL-10 immunoreactivity. Arrows indicate positively stained cells. Original magnification ×1000.

# DISCUSSION

This study demonstrates that combining calcium hydroxide with carbonate hydroxyapatite and ellagic acid modulates inflammation during pulp healing. The (CH-CHA-EA) group maintained elevated macrophage and IL-10 levels, while TNF-α was significantly reduced, particularly at later stages. In contrast, the negative control group exhibited persistent TNF-α elevation and lower IL-10, indicating ongoing inflammation. These results suggest that the combined biomaterial formulation creates an immunoregulatory environment that supports pulp tissue repair.

Macrophage expression was significantly higher in the treated groups than in the negative control from day 3 to day 14, indicating sustained macrophage presence during healing. Macrophages regulate tissue repair by resolving inflammation and promoting angiogenesis. The continued increase in macrophage expression in the (CH-CHA-EA) group suggests ongoing involvement beyond the acute phase. Macrophages secrete cytokines, growth factors, and signaling molecules that drive cellular proliferation, matrix remodeling, and tissue restoration. Thus, the enhanced macrophage response induced by carbonate hydroxyapatite and ellagic acid likely contributed to a favorable environment for pulp healing.(10)

Carbonate hydroxyapatite gradually releases calcium and phosphate ions that support cellular activity and tissue repair in the injured pulp. These ions aid in regenerating mineralized tissue and dentinogenesis, both essential for pulp healing. Carbonate hydroxyapatite also closely resembles the mineral phase of natural hard tissues and has bioactive properties that promote recovery. These features may complement the anti-inflammatory effects of ellagic acid and contribute to the improved healing seen in the (CH-CHA-EA) group.(12,13)

The cytokine profile in the (CH-CHA-EA) group may indicate changes in macrophage function during pulp healing. Macrophages are highly adaptable and can assume different phenotypes in response to local signals. Reparative macrophages are linked to inflammation resolution, tissue remodeling, and the secretion of factors that support regeneration. Although this study did not directly assess macrophage polarization, the sustained macrophage presence and anti-inflammatory cytokine profile suggest a pro-healing macrophage response in the carbonate apatite- and ellagic acid-treated group.

Persistently elevated TNF-α expression in the negative control group indicates an ongoing inflammatory response after pulp perforation. TNF-α, an early pro-inflammatory cytokine, promotes the recruitment and activation of neutrophils and monocytes, amplifying inflammation.(14) Studies show that untreated pulp exposure leads to increased inflammatory cell infiltration, tissue disorganization, necrosis, and higher TNF-α expression. Without a bioactive pulp-capping material, injured pulp remains exposed to inflammatory stimuli, maintaining TNF-α expression during healing. This aligns with the observed increase in TNF-α in NC from day 3 to day 14, indicating delayed resolution of inflammation.(15,16)

In contrast, the (CH-CHA-EA) group showed a significant reduction in TNF-α expression, especially on days 7 and 14, indicating effective regulation of inflammation during healing. This decrease coincided with increased macrophage and IL-10 expression, suggesting a coordinated immunomodulatory response. Lower TNF-α levels may reduce tissue damage and support an environment favorable for repair and regeneration. Thus, the combination of carbonate hydroxyapatite and ellagic acid appears to promote the transition from inflammation to tissue repair.

The reduced TNF-α expression in the (CH-CHA-EA) group may be due to ellagic acid's anti-inflammatory properties. Studies show that ellagic acid inhibits nuclear factor-kappa B (NF-κB) activation, which regulates pro-inflammatory cytokines such as TNF-α. Inhibiting NF-κB reduces the production of inflammatory mediators and supports inflammation resolution. Incorporating ellagic acid into the pulp-capping material likely enhanced its immunomodulatory effects and improved the healing environment. Additionally, carbonate apatite’s bioactive properties may complement ellagic acid by supporting tissue integration, mineral bioactivity, and tissue organization during healing. Together, these effects likely contributed to the reduced TNF-α expression and improved healing seen in the (CH-CHA-EA) group.(7,17)

The progressive increase in IL-10 expression during the healing period highlights its key role in resolving inflammation after pulp injury. IL-10 is a potent anti-inflammatory cytokine that limits excessive immune activation and protects tissues from inflammatory damage. In this study, the (CH-CHA-EA) group consistently showed the highest IL-10 expression at all time points, indicating a sustained anti-inflammatory response. These results suggest that carbonate hydroxyapatite and ellagic acid may help resolve inflammation and promote tissue repair.

The elevated IL-10 expression in the (CH-CHA-EA) group may be linked to the increased macrophage response during healing. Macrophages are key sources of IL-10 and regulate local immune responses by producing anti-inflammatory and pro-resolution mediators. In addition to suppressing inflammation, macrophage-derived IL-10 promotes tissue remodeling and supports the transition from inflammation to repair. The simultaneous increase in macrophage and IL-10 expression observed in this study may indicate a coordinated pro-resolution response that restores tissue homeostasis and supports pulp tissue recovery.

The highest IL-10 expression consistently corresponded with the lowest TNF-α levels, especially on days 7 and 14, suggesting coordinated regulation of inflammatory signaling. IL-10 suppresses pro-inflammatory cytokines such as TNF-α, aiding in the resolution of inflammation and maintaining tissue homeostasis. This cytokine profile is typical during the transition from inflammation to the proliferative and remodeling phases of wound healing. Thus, elevated IL-10 expression in the (CH-CHA-EA) group may have contributed to lower TNF-α levels and supported regenerative healing

The inverse relationship between IL-10 and TNF-α expression in the (CH-CHA-EA) group supports the immunomodulatory effect of the tested biomaterial. IL-10 suppresses the synthesis and release of pro-inflammatory cytokines, including TNF-α, which limits inflammatory signaling. In this study, the highest IL-10 levels coincided with the lowest TNF-α expression, particularly on days 7 and 14, indicating a regulated inflammatory response. This balance between anti-inflammatory and pro-inflammatory mediators may be important for maintaining pulp vitality and supporting tissue regeneration.

Resolution of inflammation is essential for successful regeneration, as prolonged inflammation can lead to ongoing tissue damage rather than repair. Successful pulp healing requires both the initiation and timely resolution of inflammation to prevent excessive tissue destruction.(10,18) Controlled inflammatory activity provides signals that regulate cellular recruitment, angiogenesis, extracellular matrix remodeling, and tissue repair. In this study, the coordinated increase in macrophage and IL-10 expression, along with reduced TNF-α levels, suggests that the (CH-CHA-EA) formulation promoted a regulated inflammatory environment conducive to healing. These conditions may support pulp repair and preserve pulp vitality.(19)

These findings may have important implications for vital pulp therapy and direct pulp capping. An ideal pulp-capping material should provide a protective barrier and modulate inflammation to support healing and maintain pulp vitality. The combination of calcium hydroxide, carbonate apatite, and ellagic acid promoted macrophage accumulation, increased IL-10 expression, and suppressed TNF-α expression, creating conditions favorable for pulp repair. This modified biomaterial may offer a promising strategy to improve the biological performance of pulp-capping materials and enhance regenerative pulp therapy outcomes.

# CONCLUSION

The combination of carbonate hydroxyapatite and ellagic acid with calcium hydroxide significantly modulated the inflammatory response during pulp healing following perforation. This formulation promoted macrophage accumulation, increased IL-10 levels, and reduced TNF-α expression, particularly during the later phases of healing. These findings suggest that the formulation established an immunoregulatory microenvironment conducive to inflammation resolution and tissue repair. Consequently, this modified calcium hydroxide formulation demonstrates potential for enhancing biological healing responses.

# REFERENCES

1. Qiao L, Zheng X, Xie C, Wang Y, Ye L, Zhao J, et al. Bioactive Materials in Vital Pulp Therapy: Promoting Dental Pulp Repair Through Inflammation Modulation. Biomolecules. 2025 Feb 10;15(2):258. doi:10.3390/biom15020258 PubMed PMID: 40001561; PubMed Central PMCID: PMC11853510.

2. Pohl S, Akamp T, Smeda M, Uderhardt S, Besold D, Krastl G, et al. Understanding dental pulp inflammation: from signaling to structure. Front Immunol. 2024;15:1474466. doi:10.3389/fimmu.2024.1474466 PubMed PMID: 39534600; PubMed Central PMCID: PMC11554472.

3. Kadowaki M, Yoshida S, Itoyama T, Tomokiyo A, Hamano S, Hasegawa D, et al. Involvement of M1/M2 Macrophage Polarization in Reparative Dentin Formation. Life (Basel). 2022 Nov 7;12(11):1812. doi:10.3390/life12111812 PubMed PMID: 36362965; PubMed Central PMCID: PMC9694428.

4. Anselmi C, Mendes Soares IP, Dal-Fabbro R, Chang S, de Carvalho ABG, Oliveira PHC, et al. Multifunctional bilayer scaffold for dental pulp protection and sustained calcium hydroxide release for mineralized tissue regeneration. Biomaterials. 2026 Mar 1;326:123700. doi:10.1016/j.biomaterials.2025.123700

5. Silva EJNL, Pinto KP, Riche FNSJ, Carestiato MGH, Martins JNR, Duncan HF, et al. A meta-analysis of calcium silicate-based cements and calcium hydroxide as promoters of hard tissue bridge formation. International Endodontic Journal. 2025;58(5):685–714. doi:10.1111/iej.14210

6. Widyasari R, Cahyanto A, Widyaputra S, Rachman A. Fabrication and Characterization of Carbonate Apatite-Bovine Gelatin Scaffolds for Endodontic Regeneration: A Lyophilization-Based Approach. Eur J Dent. 2025 Oct;19(4):1106–14. doi:10.1055/s-0045-1809306 PubMed PMID: 40441160; PubMed Central PMCID: PMC12494446.

7. Sari AF, Nirwana I, Yuliati A, Meizarini A, Rahayu RP, Palupi R, et al. Anti-Inflammatory Effects of Calcium Hydroxide Combined with Ellagic Acid as Pulp Capping Material: In Vivo Study. Eur J Dent. 2024 Nov 7;19(3):624–9. doi:10.1055/s-0044-1791243 PubMed PMID: 39510525; PubMed Central PMCID: PMC12182428.

8. Öngöz Dede F, Bozkurt Doğan Ş, Balli U, Durmuşlar MC, Avci B, Gülle K, et al. The effect of ellagic acid on the repair process of periodontal defects related to experimental periodontitis in rats. J Appl Oral Sci. 2021;29:e20210160. doi:https://doi.org/10.1590/1678-7757-2021-0160

9. Di Foggia M, Prati C, Gandolfi MG, Taddei P. An in vitro study on dentin demineralization and remineralization: Collagen rearrangements and influence on the enucleated phase. J Inorg Biochem. 2019 Apr;193:84–93. doi:10.1016/j.jinorgbio.2019.01.004 PubMed PMID: 30685550.

10. Li J, Jiang X, Li H, Gelinsky M, Gu Z. Tailoring Materials for Modulation of Macrophage Fate. Adv Mater. 2021 Mar;33(12):e2004172. doi:10.1002/adma.202004172 PubMed PMID: 33565154; PubMed Central PMCID: PMC9245340.

11. Damayanti H, Noordiningsih K, Wahyudi K, Hernawan, Maryani E, Yuliati A, et al. Synthesis of carbonate hydroxyapatite contained magnesium cations by dry mechano-milling. Materials Letters. 2023 May 1;338:133999. doi:10.1016/j.matlet.2023.133999

12. Ishikawa K. Bone Substitute Fabrication Based on Dissolution-Precipitation Reactions. Materials. 2010 Feb;3(2):1138–55. doi:10.3390/ma3021138

13. Zakaria MN, Cahyanto A, El-Ghannam A. Calcium release and physical properties of modified carbonate apatite cement as pulp capping agent in dental application. Biomater Res. 2018;22:35. doi:10.1186/s40824-018-0146-6 PubMed PMID: 30546914; PubMed Central PMCID: PMC6282351.

14. Wong RSY, Tan T, Pang ASR, Srinivasan DK. The role of cytokines in wound healing: from mechanistic insights to therapeutic applications. Explor Immunol. 2025 Feb 11;5:1003183. doi:10.37349/ei.2025.1003183

15. Hasan A, Roome T, Wahid M, Ansari SA, Khan JA, Jilani SNA, et al. Expression of Toll-like receptor 2, Dectin-1, and Osteopontin in murine model of pulpitis. Clin Oral Invest. 2023 Mar 1;27(3):1177–92. doi:10.1007/s00784-022-04732-2

16. He Y, Gan Y, Lu J, Feng Q, Wang H, Guan H, et al. Pulpal Tissue Inflammatory Reactions after Experimental Pulpal Exposure in Mice. J Endod. 2017 Jan;43(1):90–5. doi:10.1016/j.joen.2016.09.003 PubMed PMID: 27866710.

17. Nabil Sulyiman S, El‐Rashidy AA, El Moshy S, Abbas MMS, Waly G. Nano eggshell‐based slurry as a direct pulp‐capping material: In vitro characterization and histopathological assessment in an experimental animal model. International Endodontic Journal. 2023 Sep 1;56(9):1129–46. Located at: 169971454. doi:10.1111/iej.13949

18. Duncan HF, Cooper PR, Smith AJ. Dissecting dentine-pulp injury and wound healing responses: consequences for regenerative endodontics. Int Endod J. 2019 Mar;52(3):261–6. doi:10.1111/iej.13064 PubMed PMID: 30724394.

19. Zaky SH, Shehabeldin M, Ray H, Sfeir C, Zaky SH, Shehabeldin M, et al. The role of inflammation modulation in dental pulp regeneration. Eur Cell Mater. 2021 Feb 14;41:184–93. doi:10.22203/eCM.v041a13