Antibacterial Activity of Basil Extract and Tooth-Whitening Effect of Tomato Extract Against Streptococcus mutans and Tooth Discoloration

# Abstract

Objective. This laboratory study evaluated basil leaf extract and tomato extract, used individually and in combination, as potential natural dental materials for inhibiting Streptococcus mutans and reducing tooth discoloration. Methods. Pure S. mutans cultures and extracted permanent anterior teeth meeting the inclusion criteria were assigned to basil extract 15% and 30%, tomato extract 15% and 30%, basil-tomato combination 15% and 30%, and control groups. Antibacterial activity was assessed using the disk diffusion method. Tooth color change was assessed for seven days after coffee staining using the Vita Classical Shade Guide. Data were analyzed using Shapiro-Wilk, Mann-Whitney, Kruskal-Wallis, and Wilcoxon signed-rank tests at a significance level of p<0.05. Results. All extract groups showed significant inhibitory effects against S. mutans compared with the control group (p<0.05). For tooth discoloration, significant and more consistent color changes were observed mainly in the tomato extract groups, particularly from day 2 to day 7. Basil extract and the basil-tomato combinations did not show a stable whitening pattern. Conclusions. Basil extract demonstrated antibacterial potential against S. mutans, whereas tomato extract showed greater potential as a natural tooth-whitening agent. Combining basil and tomato extracts did not improve whitening efficacy compared with the individual extracts.

Keywords: Antibacterial agents; Basil; Dental materials; Streptococcus mutans; Tooth discoloration; Tooth whitening

# Introduction

Oral and dental health is an important component of public health because the condition of the oral cavity contributes directly to comfort, nutrition, aesthetics, quality of life, and daily productivity (1-4). Dental caries and periodontal disease remain common oral health problems in many countries despite continuous preventive and promotive strategies (5,6). Dental caries is strongly associated with enamel demineralization caused by acid production from cariogenic bacteria, especially Streptococcus mutans, after carbohydrate fermentation. Preventive approaches therefore include both mechanical plaque control and chemical control using antibacterial agents, including mouth rinses and other topical oral-care materials (3).

Interest in natural dental materials has increased because plant-derived compounds are perceived as accessible and potentially less irritating than some synthetic agents when properly formulated and tested (7). Basil leaves (Ocimum basilicum) and tomatoes (Solanum lycopersicum) are widely used natural products with relevant bioactive compounds. Basil contains essential oils, flavonoids, tannins, and eugenol, which have been associated with antibacterial activity. Tomatoes contain vitamin C, lycopene, organic acids, and peroxide-related components that may contribute to stain removal and tooth-whitening effects (8,9). These properties support their investigation as candidate natural materials for preventive and aesthetic dental applications.

Oral health problems are not limited to bacterial growth. Tooth discoloration also affects patient confidence and satisfaction with oral appearance. Extrinsic discoloration may result from coffee, tea, colored foods, tobacco, and bacterial biofilm accumulation (10). Although chemical bleaching agents are effective, inappropriate or excessive use can contribute to tooth sensitivity, gingival irritation, and enamel surface changes. Natural alternatives require laboratory testing before clinical application, especially when they are intended to combine antibacterial and whitening effects.

Previous studies have usually assessed basil or tomato extract separately and have focused on a single outcome, either antibacterial activity or tooth-whitening potential (11-14). Evidence on combinations of basil and tomato extracts remains limited. Because basil and tomato may work through different mechanisms, their combination could theoretically provide dual antibacterial and whitening functions. However, different mechanisms do not always produce synergistic effects. A direct comparison of individual and combined extracts at different concentrations is therefore needed.

This study aimed to evaluate the effectiveness of basil leaf extract and tomato extract, both individually and in combination, in inhibiting the growth of S. mutans and reducing tooth discoloration. The study also compared 15% and 30% concentrations to identify whether higher concentrations or combinations produced better antibacterial and whitening effects.

# Materials and methods

This quasi-experimental laboratory study was designed to evaluate the effectiveness of basil leaf extract and tomato extract, used individually and in combination, in inhibiting S. mutans and reducing tooth discoloration. The laboratory design allowed controlled preparation of extract concentrations, bacterial exposure, immersion conditions, and measurement procedures. The study was conducted from July to September 2025 in pharmacy, medical laboratory technology, and dental health laboratories.

The study population consisted of pure S. mutans cultures and extracted human permanent anterior teeth. Tooth samples were obtained from teeth extracted for medical reasons. The inclusion criteria were permanent anterior teeth with intact enamel surfaces and without caries, fractures, restorations, or visible structural defects. Teeth with hypoplasia, severe intrinsic staining, or enamel damage were excluded. Purposive sampling was used, and six tooth samples were assigned to each treatment group.

The independent variables were basil leaf extract and tomato extract at different concentrations, either individually or in combination. The treatment groups were basil extract 15% (EK15), basil extract 30% (EK30), tomato extract 15% (ET15), tomato extract 30% (ET30), basil 15% + tomato 15% combination (Comb15), basil 30% + tomato 30% combination (Comb30), and a control group. The dependent variables were inhibition-zone diameter for S. mutans growth and tooth color change after treatment.

Basil leaves and tomatoes were processed by maceration using 96% ethanol. The filtrate was evaporated to obtain concentrated extracts, which were then diluted to the required concentrations. Antibacterial activity was assessed using the disk diffusion method. Sterile disks containing each extract preparation were placed on culture media inoculated with S. mutans, and inhibition zones were measured in millimeters after incubation. Larger inhibition zones indicated greater antibacterial activity.

For tooth discoloration assessment, selected teeth were first stained by immersion in coffee solution for ten days. Each stained tooth was then immersed in the corresponding extract solution and observed for seven consecutive days. Tooth color was assessed at the middle third of the tooth surface using the Vita Classical Shade Guide before and after treatment. Greater shade change indicated a stronger whitening effect.

Ethical approval was obtained from the Health Research Ethics Commission of the Ministry of Health, Jambi, under protocol number LB.02.06/5/1148/2025. All procedures involving extracted human teeth followed established ethical standards for human tissue research. No identifiable patient images or personal data were used.

Data were analyzed using SPSS. The Shapiro-Wilk test was used to assess normality. Because several variables were not normally distributed, non-parametric tests were applied. The Mann-Whitney test compared treatment groups with the control group, the Kruskal-Wallis test compared multiple treatment groups, and the Wilcoxon signed-rank test compared pre- and post-treatment tooth color values within each group. Statistical significance was set at p<0.05.

# Results

The Shapiro-Wilk test showed that several pre-treatment and post-treatment data points were not normally distributed across the treatment and control groups (Table 1). Therefore, non-parametric statistical tests were used for subsequent analyses.

The Mann-Whitney test showed that all extract groups had significant antibacterial effects against S. mutans compared with the control group (Table 2). The Kruskal-Wallis test also indicated significant differences among the extract groups in their ability to inhibit bacterial growth (Table 3). These findings suggest that both extract type and concentration influenced antibacterial activity.

Tooth color changes during the seven-day observation period are presented in Table 4. The tomato extract groups showed a more consistent trend of color improvement than the basil extract and combination groups. The Wilcoxon signed-rank test showed that significant pre-post color changes occurred mainly in the tomato extract groups, particularly from day 2 to day 7 (Table 5).

The Mann-Whitney comparisons between each treatment group and the control group showed that tomato extract produced the most frequent significant differences in tooth discoloration outcomes (Table 6). Basil extract and the basil-tomato combinations did not show consistent differences compared with the control. The Kruskal-Wallis test further showed significant differences among groups from day 3 to day 7 (Table 7), indicating that whitening effects became more apparent after repeated exposure rather than immediately after treatment.

# Discussion

This study evaluated the antibacterial and tooth-whitening potential of basil leaf extract and tomato extract as natural dental material candidates. The first objective was achieved because all treatment groups showed significant inhibitory effects against S. mutans compared with the control group. However, the second objective was only partly achieved. Consistent tooth-whitening effects were observed mainly in the tomato extract groups, whereas basil extract and the basil-tomato combinations showed limited and inconsistent whitening effects.

The antibacterial results support the biological plausibility of basil and tomato extracts as oral-care materials. Basil contains eugenol, flavonoids, tannins, and other phenolic compounds that may disrupt bacterial cell membranes, denature proteins, and inhibit enzymes involved in bacterial metabolism (8,9,17,18). Tomato extract may also contribute antibacterial activity through acidic and antioxidant compounds, although its main relevance in this study was whitening potential. The significant antibacterial activity observed in the combination groups indicates that combining the extracts did not reduce their ability to inhibit S. mutans.

The whitening results showed a different pattern. Tomato extract, both at 15% and 30%, produced more stable tooth color changes across the observation period. This finding is consistent with previous reports that tomatoes may contribute to tooth-whitening effects because of their peroxide-related and acidic components, which can assist in breaking down extrinsic stains (15,16,19). In contrast, basil extract did not consistently reduce discoloration, which is reasonable because its active compounds are primarily antibacterial rather than oxidative whitening agents.

The lack of superior whitening performance in the combination groups suggests that antibacterial activity and whitening activity do not necessarily increase together. A formulation may be effective against S. mutans but ineffective for stain oxidation. Basil compounds may not directly support the oxidative degradation of pigments, and their combination with tomato extract may dilute or interfere with the whitening components of tomato. This finding is important because natural ingredient combinations should not be assumed to be synergistic unless their mechanisms are compatible and empirically confirmed.

These findings have practical implications for the development of herbal oral-care materials. Basil extract may be more suitable for antibacterial applications, whereas tomato extract may be more relevant for natural tooth-whitening formulations. A two-step formulation may be more appropriate than a single combined product if antibacterial and whitening actions require different active mechanisms. The results also support further investigation of local natural products as preventive and aesthetic dental materials.

This study has several limitations. The sample size was relatively small, which may limit generalizability. The in vitro laboratory setting did not fully reproduce the oral environment, including saliva, pH fluctuation, pellicle formation, and multispecies biofilms. Tooth whitening was assessed using a static immersion method and a shade guide rather than digital colorimetry. In addition, the active compounds in the extracts were not quantitatively characterized. Future studies should include chemical standardization, enamel surface analysis, larger samples, and clinical or simulated oral-environment testing.

# Conclusions

Basil leaf extract and tomato extract, used individually or in combination, inhibited the growth of S. mutans under laboratory conditions. Basil extract demonstrated antibacterial potential, whereas tomato extract showed stronger and more consistent tooth-whitening potential. The basil-tomato combinations did not improve whitening efficacy compared with tomato extract alone. These findings suggest that basil and tomato extracts may be developed for different natural oral-care applications, but further formulation and clinical studies are required before routine dental use.

# AI use disclosure

The authors used ChatGPT by OpenAI for language editing, journal-format adjustment, and readability improvement. All scientific content, data, interpretations, and references were reviewed and approved by the authors, who assume full responsibility for the final manuscript.

# References

1. Baiju RM, Peter E, Varghese NO, Sivaram R. Oral health and quality of life: current concepts. J Clin diagnostic Res JCDR. 2017;11(6):ZE21.

2. Subramaniam P, Girish Babu KL. Effect of herbal agents on Streptococcus mutans: A review of literature. J Nat Sci Biol Med. 2014;5(2):359–65.

3. Ali M, Chaudhary N. Herbal alternatives in tooth whitening: A systematic review of natural bleaching agents. J Herb Med. 2021;27:100427.

4. Spanemberg JC, Cardoso JA, Slob E, López-López J. Quality of life related to oral health and its impact in adults. J Stomatol oral Maxillofac Surg. 2019;120(3):234–9.

5. Kharisma AD, Lestari D. Kandungan fitokimia tomat dan potensinya sebagai agen pemutih gigi alami. J Farm Indones. 2020;12(3):150–7.

6. Dewi SP, Hartanti AT. Pengaruh ekstrak tomat (Solanum lycopersicum) terhadap perubahan warna gigi. J Mater Kedokt Gigi Indones. 2019;8(2):23–9.

7. Hendarmin H, Suwargiani AA, Widyarman AS. Exploring the potential of tomato (Solanum lycopersicum) extract patch for tooth bleaching: An in-vitro study. Int J Dent Oral Heal. 2024;10(1):22–9.

8. Kharisma AD, Lestari D. Phytochemical constituents and antibacterial activity of Ocimum basilicum against oral pathogens: A systematic review. Pharmacogn Rev. 2020;14(28):75–82.

9. Fani M, Kohanteb J. In vitro antimicrobial activity of Ocimum basilicum and Ocimum sanctum essential oils against Streptococcus mutans. J Dent. 2017;18(4):210–6.

10. Zhakipbekov K, Atazhanova G, Dukenbayeva A, Kudaibergenov S. Ocimum basilicum L.: Chemical composition and biological activities—A comprehensive review. Molecules. 2024;29(5):1121.

11. de Aguiar AC, de Lima Damasceno BPG, da Silva L. Antimicrobial activity of selected essential oils against oral pathogens. J Appl Oral Sci. 2018;26:e20160479.

12. Syahrul A, Syahriel M. Efektivitas ekstrak kemangi (Ocimum basilicum) terhadap Streptococcus mutans penyebab karies gigi: Kajian laboratorium. J Penelit Kesehat. 2021;19(2):101–9.

13. Bayala B, Bassolé IHN, Scifo R, Gnoula C, Morel L, Lobaccaro JMA, et al. Antioxidant, anti-inflammatory and antiproliferative activities of essential oils of plants used in traditional medicine in Burkina Faso. PLoS One. 2014;9(12):e113691.

14. Strużycka I. The oral microbiome in dental caries. Polish J Microbiol. 2014;63(2):127.

15. Mulky MJ, Kamath AT, Hedge MN. Effect of tomato extract on tooth stains: An in vitro study. J Clin Diagnostic Res. 2014;8(6):45–8.

16. Abdullah R. Tomato extract as a natural bleaching agent: An in-vitro study. J Oral Biol. 2021;8(2):45–52.

17. Astuti R, Nurjanah S, Rachmawati D. Aktivitas antibakteri ekstrak daun kemangi (Ocimum basilicum) terhadap Streptococcus mutans. J Kesehat Gigi. 2016;3(1):18–25.

18. Ningrum RP, Waznah L. Daya hambat ekstrak daun kemangi terhadap pertumbuhan Streptococcus mutans. J Kesehat Masy Andalas. 2018;12(1):33–8.

19. Benahmed AG, Gasmi A, Menzel A, Hrynovets I, Chirumbolo S, Shanaida M, et al. A review on natural teeth whitening. J oral Biosci. 2022;64(1):49–58.

20. Fani M, Kohanteb J. In vitro antibacterial activity of Ocimum basilicum and Ocimum sanctum essential oils against Streptococcus mutans. J Dent. 2017;18(4):210–6.

21. Sharma A, Rajput R. Phytochemical analysis and antibacterial activity of Ocimum basilicum L. Int J Pharm Sci Rev Res. 2016;38(1):66–70.

# Tables

Table 1. Shapiro-Wilk normality test for pre-treatment and post-treatment tooth color values in basil, tomato, combination, and control groups.

| Days | n | EK15 (Sig.) | EK30 (Sig.) | ET15 (Sig.) | ET30 (Sig.) | Comb15 (Sig.) | Comb30 (Sig.) | K (Sig.) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Pre | 6 | 0.212 | 0.101 | 0.167 | 0.000 | 0.004 | 0.475 | 0.421 |
| Day 1 | 6 | 0.421 | 0.473 | 0.421 | 0.212 | 0.001 | 0.11 | 0.167 |
| Day 2 | 6 | 0.167 | 0.167 | 0.473 | 0.167 | 0.212 | 0.11 | 0.035 |
| Day 3 | 6 | 0.421 | 0.421 | 0.035 | 0.006 | 0.004 | 0.033 | 0.101 |
| Day 4 | 6 | 0.101 | 0.167 | 0.415 | 0.035 | 0.091 | 0.091 | 0.212 |
| Day 5 | 6 | 0.252 | 0.473 | 0.07 | 0.415 | 0.212 | 0.101 | 0.001 |
| Day 6 | 6 | 0.415 | 0.091 | 0.96 | 0.004 | 0.001 | 0.091 | 0.212 |
| Day 7 | 6 | 0.035 | 0.101 | 0.035 | 0.006 | 0.473 | 0.212 | 0.212 |

Table 2. Mann-Whitney test comparing extract groups with the control group for inhibition of Streptococcus mutans.

| Groups | n | Significance (p) |
| --- | --- | --- |
| Basil extract 15% | 4 | 0.018 |
| Basil extract 30% | 4 | 0.018 |
| Tomato extract 15% | 4 | 0.017 |
| Tomato extract 30% | 4 | 0.017 |
| Basil + tomato combination 15% | 4 | 0.018 |
| Basil + tomato combination 30% | 4 | 0.018 |

Table 3. Kruskal-Wallis test among extract groups for inhibition of Streptococcus mutans.

| Groups | n | Significance (p) |
| --- | --- | --- |
| EK15, EK30, ET15, ET30, Comb15, Comb30 | 4 per group | 0.001 |

Table 4. Mean difference and standard deviation of tooth color changes during the seven-day observation period.

| Days | n | EK15 (Mean±SD) | EK30 (Mean±SD) | ET15 (Mean±SD) | ET30 (Mean±SD) | Comb15 (Mean±SD) | Comb30 (Mean±SD) | Control (Mean±SD) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Day 1 | 6 | 0.42 ± 1.40 | 0.25 ± 0.75 | 0.50 ± 1.20 | 0.42 ± 0.90 | 0.17 ± 0.58 | 0.25 ± 0.75 | 0.17 ± 1.30 |
| Day 2 | 6 | 0.58 ± 1.10 | 0.17 ± 1.30 | 1.00 ± 1.20 | 0.58 ± 1.20 | 0.33 ± 1.10 | 0.33 ± 1.80 | 0.33 ± 1.20 |
| Day 3 | 6 | 0.08 ± 1.10 | 0.33 ± 1.30 | 1.00 ± 1.30 | 0.75 ± 1.10 | 0.08 ± 0.79 | 0.33 ± 1.50 | 0.17 ± 0.98 |
| Day 4 | 6 | 0.33 ± 0.65 | 0.17 ± 1.03 | 1.42 ± 1.60 | 1.00 ± 1.04 | 0.25 ± 0.75 | 0.67 ± 1.07 | 0.17 ± 0.98 |
| Day 5 | 6 | 0.17 ± 1.70 | 0.08 ± 1.40 | 1.83 ± 1.50 | 1.33 ± 1.50 | 0.58 ± 0.99 | 0.92 ± 1.40 | 0.50 ± 1.40 |
| Day 6 | 6 | 0.42 ± 1.60 | 0.50 ± 1.20 | 1.67 ± 2.10 | 1.33 ± 1.56 | 0.58 ± 1.24 | 1.00 ± 1.60 | 0.33 ± 1.50 |
| Day 7 | 6 | 0.50 ± 1.10 | 0.67 ± 0.78 | 1.25 ± 1.42 | 1.33 ± 1.50 | 0.08 ± 1.24 | 0.75 ± 0.97 | 0.33 ± 1.03 |

Table 5. Wilcoxon signed-rank test comparing pre-treatment and post-treatment tooth color values in each group.

| Days | n | EK15 | EK30 | ET15 | ET30 | Comb15 | Comb30 | Control |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Day 1 | 6 | 0.395 | 0.317 | 0.163 | 0.157 | 0.317 | 0.317 | 0.564 |
| Day 2 | 6 | 0.102 | 1.000 | 0.026 | 0.129 | 0.414 | 0.672 | 0.48 |
| Day 3 | 6 | 1.000 | 0.197 | 0.041 | 0.039 | 1.000 | 0.705 | 0.655 |
| Day 4 | 6 | 0.157 | 1.000 | 0.039 | 0.026 | 0.564 | 0.098 | 0.317 |
| Day 5 | 6 | 0.915 | 0.655 | 0.026 | 0.027 | 0.046 | 0.071 | 0.334 |
| Day 6 | 6 | 0.396 | 0.157 | 0.042 | 0.026 | 0.102 | 0.059 | 0.516 |
| Day 7 | 6 | 0.194 | 0.014 | 0.038 | 0.034 | 0.783 | 0.038 | 0.414 |

Table 6. Mann-Whitney test comparing extract groups with the control group for tooth discoloration.

| Days | n | EK15 | EK30 | ET15 | ET30 | Comb15 | Comb30 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Day 1 | 6 | 0.459 | 0.665 | 0.323 | 0.309 | 0.923 | 0.665 |
| Day 2 | 6 | 0.456 | 0.682 | 0.065 | 0.456 | 1.000 | 0.869 |
| Day 3 | 6 | 0.611 | 0.266 | 0.029 | 0.054 | 0.924 | 0.432 |
| Day 4 | 6 | 0.859 | 0.73 | 0.012 | 0.021 | 0.665 | 0.246 |
| Day 5 | 6 | 0.411 | 0.452 | 0.157 | 0.07 | 0.867 | 0.321 |
| Day 6 | 6 | 0.8 | 0.738 | 0.023 | 0.025 | 0.456 | 0.121 |
| Day 7 | 6 | 0.614 | 0.105 | 0.026 | 0.02 | 0.458 | 0.18 |

Table 7. Kruskal-Wallis test among basil and tomato extract groups for tooth discoloration.

| Days | n | Significance (p) |
| --- | --- | --- |
| Day 1 | 6 | 0.792 |
| Day 2 | 6 | 0.37 |
| Day 3 | 6 | 0.022 |
| Day 4 | 6 | 0.006 |
| Day 5 | 6 | 0.018 |
| Day 6 | 6 | 0.035 |
| Day 7 | 6 | 0.014 |

# Figure legends

No figures are included in this manuscript.