Optimizing Dental Composites: Investigating the Impact of Bemban (Donax canniformis) Fiber on Mechanical Strength Parameters

Agung Satria Wardhana*, Gigih Nur Ifani Yusro**, Adelvia Pramudita Balqis**, Debby Saputera***, Bayu Indra Sukmana***

* Faculty of Dentistry, Department of Dental Material, Lambung Mangkurat University

** Faculty of Dentistry, Lambung Mangkurat University

*** Faculty of Dentistry, Department of Prosthodontics, Lambung Mangkurat University

**** Faculty of Dentistry, Department of Dental Forensics, Lambung Mangkurat University

Correspondence: agung.wardhana@ulm.ac.id

Keywords:

Composite resin, Nanohybrid, Diametral tensile strength, Flexural strength, Bemban fiber (Donax canniformis).

ABSTRACT

Background: Nanohybrid composite resin is a dental restoration material with good aesthetics, but is at risk of fracture due to masticatory pressure and improper polymerization. The addition of bemban (Donax canniformis) fibers containing cellulose and lignin can be an economical and environmentally friendly alternative reinforcement. Objective: This study aimed to analyze the effect of bemban (Donax canniformis) fiber addition in improving the diametral tensile strength and flexural strength of nanohybrid composite resins. Methods: This experimental study used 21 samples divided into 3 groups: nanohybrid composite resins without fibers, with bemban fibers, and with polyethylene fiber. The samples were immersed in saline solution, incubated (24 hours, 37°C), and then tested for tensile strength and flexural strength using a Universal Testing Machine). Results: In the diametral tensile strength test, there was a significant difference between the three groups. While in the flexural strength test there was only a significant difference between group 2 and group 3. In both tests, the group with the addition of polyethylene fiber had the highest strength value. Conclusion: The addition of bemban fibers affects the diametral tensile strength and flexural strength. And only the diametral tensile strength test can increase the diametral tensile strength of the nanohybrid composite resin.

BACKGROUND

Data from the Survei Kesehatan Indonesia (SKI) in 2023 showed that 43.6% of the Indonesian population experienced dental and oral problems, including cavities.1 The use of composite resins, such as nanohybrid composite resins, is one solution. Nanohybrid composite resins contain fillers with mixed sizes, namely fillers measuring 20-75 nm, filler particles measuring 0.4-5 µm, and silica or zirconia nanocluster fillers measuring 2-20 nm.2

Dental restoration materials need to consider their mechanical properties, namely diametral tensile strength and flexural strength. Flexural strength relates to the resistance of a material to forces that describe the pressure distribution under masticatory load.3 While diametral tensile strength relates to the ability of a material to withstand forces that cause elongation before fracture.4 Fracture can be triggered by various factors, such as excessive masticatory pressure, suboptimal polymerization process, and habits such as bruxism.5,6 One way to improve the mechanical properties of restoration materials is to add a fiber layer to the composite resin.7

The use of fibers has several benefits, such as increasing strength, stiffness, and resistance to fracture.8 Based on the type, fibers are divided into two categories, namely synthetic fibers and natural fibers.9 One fiber that is often used is polyethylene fiber, which has superior strength compared to glass fiber.10, However, polyethylene fiber has several disadvantages, such as self-abrasive properties, low modulus of elasticity, and carbon compound (C) content which is moderately cytotoxic to fibroblast cells.11 As an alternative, natural fibers can be used to increase the mechanical strength of composite resins.9

Bemban (Donax canniformis) is a plant with natural fibers that can be found in wetland areas.12 Bemban fibers have three main components: moisture content of 2.36%, cellulose content of 22.52%, and lignin content of 1.33%.13 The cellulose structure is formed from fibrils bonded together through hydrogen bonds, which gives bemban fibers strong and flexible characteristics.14 Meanwhile, lignin is an organic compound with a complex structure located in the cell wall, which functions to provide strength to the plant and helps its resistance to external environmental conditions.13

Based on the above reasons, there has been no research on the addition of bemban (Donax canniformis) fibers to composite resin filling materials. Research is needed on the effect of the addition of bemban (Donax canniformis) fibers on the diametral tensile strength and flexural strength values of nanohybrid composite resins.

RESEARCH METHOD .

Ethical Clearance

This research protocol was approved by the Ethics Committee of the Faculty of Dentistry, Lambung Mangkurat University (No. 009/KEPKG-FKGULM/EC/VII/2024).

Materials

The materials used in this study were nanohybrid type composite resin (3M™ Filtek™ Z250 XT Nano Hybrid Universal), synthetic polyethylene fiber (Infibra®), primary (bonding) material (3M™ Single Bond Universal Adhesive), bemban fiber (Donax canniformis), and saline solution.

Preparation of Bemban Fiber

Bemban stems were selected with a diameter criteria of 4-5 cm, cleaned, cut ±20 cm, and split into 2. The bemban stems were boiled for ±60 minutes, then dried in the sun until the moisture content of the bemban stems was reduced. Next, a wire brush was used to remove the cork layer attached to the fibers. Then, the bemban fibers were decomposed into fiber strands. Next, the bemban fiber strands are placed on a glass plate and treated with bonding before being applied to the mold.15

Preparation of Polyethylene Fiber

Polyethylene fiber is decomposed one by one into fiber strands, placed on a glass plate, and polyethylene fiber strands are dabbed with bonding material before being applied into the mold.

Sample Preparation

The diametral tensile strength test consisted of 21 samples and the flexural strength test consisted of 15 samples divided into 3 groups. Group 1 nanohybrid composite resin with polyethylene fiber, group 2 nanohybrid composite resin without fiber, and group 3 nanohybrid composite resin with bemban fiber.

The diametral tensile strength test used a mold with a diameter of 6 mm and a thickness of 3 mm (ADA No.27) and the flexural strength test used a 25x2x2 mm mold. 3M™ Filtek™ Z250 XT Nano Hybrid Universal composite resin was applied to the mold up to ½ the height of the sample. The processed bemban fibers were placed on top of the first layer composite resin using tweezers in a horizontal position. The fibers were placed at a height of ½ of the sample with a unidirectional fiber orientation. Next, the fiber layer was covered using 3M™ Filtek™ Z250 XT Nano Hybrid Universal composite resin until the height covered the entire sample. Condensation was carried out using a condenser and irradiated for 20 seconds with the closest possible beam distance or 1 sheet of celluloid tape.15,16 Light curing was carried out on both sides of the composite resin sample.

Storage in Incubator

The finished composite resin molds were then stored in an incubator using a conical tube and immersed in saline solution at 37°C for 24 hours.15

Diametral Tensile Strength and Flexural Strength Testing

The samples were tested with a Universal Testing Machine with a crosshead speed of 0.5 mm/min and a load of 5 kN. The diametral tensile strength test was conducted by placing the sample in the center diametrically just below the load guide needle. While the flexural strength test was carried out by placing the sample on the test equipment with a bending span of 20 mm, loading the piston perpendicular to the width of the fiber. Then the sample is tested until it breaks into two parts. Data collection is done by looking at the number that appears on the test equipment monitor which shows the amount of load in a certain number (N).4

Data Analysis

The data obtained were evaluated statistically by performing the Shapiro-Wilk normality test and Levene's test for homogeneity. Furthermore, parametric analysis was carried out using the One Way Anova hypothesis test and the Bonferroni Post Hoc test to analyze the significance between groups.

RESULTS

Diametral Tensile Strength of Nanohybrid Composite Resins

The visualization of the final results of the diametral tensile strength test is shown in Figure 1. The diametral tensile strength value of group 1 was lower than that of group 2 and group 3 (p=0.000; p=0.005). The diametral tensile strength values of group 2 were higher than those of group 1 and group 3 (p=0.000; p=0.017).

Figure 1. Results of Diametral Tensile Strength Value of Nanohybrid Composite Resin. The characters above the bar show the group difference siginification (p<0.05). Group 1, no treatment; Group 2, polyethylene fiber; Group 3, bemban fiber.

Flexural Strength of Nanohybrid Composite Resins

Visualization of the final results of the flexural strength assessment is shown in Figure 3. The flexural strength value of group 1 was lower than that of group 2 (p=0.320). The diametral tensile strength values of group 2 were higher than those of group 1 and group 3 (p=0.480; p=0.021).

Figure 2. Results of flexural strength values of nanohybrid composite resin. Characters above the bar show group difference siginification (p<0.05). Group 1, no treatment; Group 2, polyethylene fiber; Group 3, bemban fiber.

DISCUSSION

Based on the research, it shows that group 1 in the form of composite resin which is carried out diametral tensile strength test without the addition of fiber shows a mean value of 34.565 Mpa, while the flexural strength test shows a mean value of 92.498 Mpa. The value in group 1 of the diametral tensile strength test was significant to groups 2 and 3 (p=0.000 and p=0.005), while the value in the flexural strength test was not significant to group 2 and group 3 (p=0.320 and p=0.480). Group 1 is the group with lower dimetral and flexural tensile strength values compared to the group with synthetic fiber added. This is in line with the research of Ananda, et al (2018) which states that the flexural strength of bulk fill composite resins without added fibers is lower than that of those with synthetic fibers (glass fiber) added.17

Composite resins without added fibers have lower strength compared to composite resins containing fibers. This is due to the role of fiber as a supporting material that can increase the strength and stiffness of the composite resin against fracture. Fiber has a modulus of elasticity that is almost the same as the modulus of elasticity of dentin tissue, so it is able to absorb pressure, reduce shrinkage, and distribute pressure evenly throughout the composite resin. Thus, the risk of fracture in the composite resin can be minimized.8,18

Based on the research shows that group 2 in the form of composite resins conducted diametral tensile strength test with the addition of polyethylene fiber showed a mean value of 50.182 Mpa, while the flexural strength test showed a mean value of 110.047 Mpa. The value in group 2 of the diametral tensile strength test was significant to groups 1 and 3 (p=0.000 and p=0.017), while the value in the flexural strength test was significant to group 3 (p=0.021) and not significant to group 1 (p=0.320). Group 2 was the group with the highest dimetral and flexural tensile strength values compared to the other groups. This is in line with the research of Nabilah, et al (2016) which states that polyethylene fiber can increase the flexural strength of microhybrid composite resins.19

Polyethylene fiber has an organized pattern with a braided design that is able to lock the fibers well so as to increase the resistance, stability, and shear strength between fibers to prevent cracking.20 Theoretically, polyethylene is a repeating structure of ethylene monomers (C₂H₄).21 Polyethylene is formed through the ethylene polymerization process which produces long chains of ethylene monomers.22 In this study, the type of polyethylene fiber used was Infibra®, which belongs to the ultra high molecular weight polyethylene (UHMWPE) category.23 UHMWPE has superior characteristics, such as wear resistance, high ductility, and good biocompatibility.24 These advantages are due to several factors: (1) UHMWPE fibers have a molecular weight between 3.1 to 6 million g/mol and consist of more than 100,000 ethylene units with a very high linear orientation in the straight chain structure; (2) the molecules have non-polar symmetry without side chains, so intermolecular forces are minimal; (3) the polyethylene molecular chain has excellent flexibility and molecular regularity.24,25

Furthermore, group 3 in the form of composite resins that were tested for diametral tensile strength with the addition of bemban fibers showed a mean value of 42.999 Mpa. This group was significant to groups 1 and 2 (p=0.005 and p=0.017). Group 3 with this test is a group with a higher dimetral tensile strength value compared to group 1 without added fiber, but lower than group 2 which added synthetic fiber (polyethylene fiber). This is in line with the research of Hernandi, et al (2018) which states that bagasse fiber (Saccharum Officinarum L.) can increase the diametral tensile strength of nanohybrid composite resins.15

Compositional analysis shows that bemban (Donax canniformis) fibers contain 2.36% water, 22.52% cellulose, and 1.33% lignin.13 The cellulose component is formed from photosynthesized glucose units, which are arranged in a highly organized microfibril structure that produces stiffness, biocompatibility, and strength.9,26 Lignin functions as a binding matrix that allows plants to maintain their upright structure.9 Lignin is a polymer with a three-dimensional structure that has high hydrolysis resistance and durability.26 The bemban fibers in composite resins are arranged in a unidirectional manner, where the fibers are oriented parallel in the same direction. This method shows advantages over random orientation as it has fewer gaps between fibers.27 When tested, fibers with unidirectional orientation performed better in various aspects, including diametral tensile strength, impact strength, coefficient of thermal expansion, and thermal conductivity, compared to measurements from different directions.16 The next factor is the combination of composite resin, fiber, and silane as a coupling agent. Silane plays a role in forming a strong and durable bond between the composite resin and the fiber by generating siloxane (Si-O-Si) bonds with hydroxyl (C=O) groups on the fiber surface, which then interacts with functional groups in the composite resin as illustrated in Figure 3.28 The use of coupling agents on fibers can improve the ability of fibers to wet the matrix (wet ability), surface roughness, surface energy, and strengthen the interfacial bond between fibers and matrix.16

Figure 3 Illustration of bonding between composite resin and fiber with siloxane (Si-O-Si) bonding together with hydroxyl (C=O) groups in bemban fiber.28,29

Based on the study, it shows that group 3 in the form of composite resin which is tested for flexural strength with the addition of bemban fiber shows a mean value of 77.424 Mpa. This group was significant to group 2 (p=0.021) and not significant to group 1 (p=0.480). Group 3 with this test is the group with the lowest value compared to the other groups. This is in line with the research of Agunsoye, et al (2019) which shows that the addition of fiber will have no effect in increasing mechanical strength if the bond between the matrix and fiber is not strong enough.30

A possible factor causing the non-increase in flexural strength in group 3 is the uncontrolled state of the sample, one of which is the entry of water into the sample due to the presence of bemban fibers contaminated with water before being inserted into the mold. This can occur during the research process due to the lack of maximum drying or drying of bemban fibers.In the research of Kumar, et al (2021), the decrease in mechanical properties is related to the degradation of the polymer matrix and reinforcing filler particles caused by water which results in the detachment of the filler-resin interface bond causing the flexural strength to decrease.31 In addition, the coating on the bemban fiber also affects the increase in the flexural strength of the composite resin.In the research of Rezvani, et al (2015) explained that fibers with greater thickness can increase the flexural strength value of the composite resin itself.32

Another factor that can cause a decrease in flexural strength is porosity. Porosity occurs when air is trapped in the material during the stirring or molding process. There are several causes of porosity, such as imperfect bonding between fiber and matrix, moisture contamination from the tools used, and water absorption from the material itself during the manufacturing process.The presence of porosity causes the applied load to be unevenly distributed on the material, which in turn will affect the overall flexural strength.30

CONCLUSION

Based on the results of this study, it can be concluded that the addition of bemban fiber can increase the diametral tensile strength value of nanohybrid composite resin, but it is still lower than polyethylene fiber. While the addition of bemban fiber in flexural strength testing does not increase the strength value. The researcher suggested that further research be carried out regarding the procedure for making bemban fibers in order to increase diametral and flexural tensile strength, the application of fibers with other orientations, and further research related to the toxicity of materials.

ACKNOWLEDGEMENT

The researcher expresses his deepest gratitude to Allah SWT. because by His grace, the researcher can complete the research well and on time. To all supervisors and examiners who have provided advice and input. And do not forget to thank all friends who have provided moral and material support so that this research can be completed on time.

REFERENCES

1.	Kementerian Kesehatan RI. Survei Kesehatan Indonesia.; 2023.

2.	Nu’ma JA. Perbedaan Kekuatan Tekan Antara Resin Komposit Nanofiller dan Resin Komposit Nanohybrid dengan Teknik Bulk Fill. Sci Dent J. 2019;1(2):1-15.

3.	Al-Idrus SMF, Arifin J, Herlina F. Perbandingan Komposit Polyester Serat Bemban (Donax canniformis), Timbaran, dan Bilaran Terhadap Kekuatan Impak Dan Bending. Dr Diss Univ Islam Kalimantan MAB. Published online 2020:1-4.

4.	Suparno NR, Nabila AS. Pengaruh Ph Saliva Terhadap Kekuatan Tarik Diametral Resin Komposit Nanohybrid. B-Dent J Kedokt Gigi Univ Baiturrahmah. 2023;10(1):1-8. doi:10.33854/jbd.v10i1.941

5.	Wita Bancin UA, Erlita I, Diana S. Pengaruh Jarak Penyinaran Terhadap Nilai Derajat Konversi Resin Komposit Bioaktif. Dentin. 2022;6(2):82-86. doi:10.20527/dentin.v6i2.6391

6.	Thayer MLT, Ali R. The dental demolition derby: bruxism and its impact - part 3: repair and reconstruction. Br Dent J. 2022;232(11):775-782. doi:10.1038/s41415-022-4293-8

7.	Thamara CA, Erlita I, Diana S, Et.all. The Effect of Bagasse Fiber (Saccharum officinarum L.) Addition on the Compressive Strength of Bulk Fill Composite Resin. Dentino J Kedokt Gigi. 2018;III(1):72-75.

8.	Puspita S, Soesilo D, Rochyani L, Cevanti TA. Perbandingan daya antibakteri serat selulosa sabut kelapa (Cocos nucifera L.) pada konsentrasi berbeda terhadap Streptococcus mutan. (Comparison of the antibacterial power of coconut cellulose fiber). J Kedokt Gigi Univ Padjadjaran. 2022;34(1):51. doi:10.24198/jkg.v34i1.35076

9.	Murdiyanto D. Potensi Serat Alam Tanaman Indonesia Sebagai Bahan Fiber Reinforced Composite Kedokteran Gigi. J Mater Kedokt Gigi. 2017;6(1):14. doi:10.32793/jmkg.v6i1.260

10.	Astuti NKA, Sumantri, Kusumayanti KS. The Effect of Reinforced Polyethylene Fiber on Flowable Resin Composite as Splinting Material on Attachement of Streptoccocus Mutans. Interdental J Kedokt Gigi. 2022;18(1):1-7. doi:10.46862/interdental.v18i1.3758

11.	Murdiyanto D, Andrian DS. Evaluasi Sitotoksisitas Serat Daun Nanas (Ananas comosus (L.) Merr) dan Polyethylene Sebagai Fiber Reinforced Composite. B-Dent J Kedokt Gigi Univ Baiturrahmah. 2019;6(2):126-131. doi:10.33854/jbd.v6i2.263

12.	Setyawati A, Krisdianto K, Nisa C. Pertumbuhan Bamban (Donax canniformis) di Jejangkit Muara, Kabupaten Barito Kuala, Provinsi Kalimantan Selatan. Bioscientiae. 2022;19(1):52-66. doi:10.20527/b.v19i1.5102

13.	Saputra Y, Zahara AWL, Lazuardi MA, Nur, Amada MS, Haryanti NH. Karakteristik Aspal Porus dengan Campuran Serat Bemban (Donax Canniformis) Terhadap Porositas, Void In Mixture, dan Marshall Quotient. J Sci Appl Technol. 2023;7(1):26. doi:10.35472/jsat.v7i1.1086

14.	Murdiyanto D, Kristi RMB. Pengaruh Penambahan Serat Daun Nanas (Ananas comosus (L.) Merr) Terhadap Kekuatan Tekan Resin Komposit Flowable. JIKG (Jurnal Ilmu Kedokt Gigi). 2020;3(1):5-9.

15.	Erlita I, Hernandi YM, Nahzi MYI. Effect Of Diametral Tensile Strength Of Bulk Fill Composite Resin With The Addition Of Sugarcane Waste Fiber. Dentino J Kedokt Gigi. 2018;III(1):43-46.

16.	Dendy Murdiyanto AHA. Pengaruh Penambahan Serat Kepompong Ulat Sutra (Bombyx moril.) Terhadap Kekuatan Tarik Diametral Resin Komposit Flowable. JIKG (Jurnal Ilmu Kedokt Gigi). 2020;3(2):14-18.

17.	Ananda SFR, IsyanaErlita, D.H. I. the Effect of Bagasse Fiber Addition in Flexural Strength of Bulk Fill Composite Resin. Dentino J Kedokt Gigi. 2018;III(1):72-75.

18.	Mahardika C, Hernawatiningsih H, Kristanti Y, Mulyawati E. Restorasi Onlay Komposit Pasca Perawatan Endodontik Pada Gigi Molar Pertama Kanan Atas : Laporan Kasus. E-Prodenta J Dent. 2022;6(1):611-616. doi:10.21776/ub.eprodenta.2022.006.01.9

19.	Nabilah VZ, Hidayati L, Sumono A. Flexural Strength of Microhybrid Composite Resin with Polyethylene Fiber’s Layer Addition. Proccedings B FORKINAS. 2016;4(June):2016.

20.	Panjaitan FE, Paramakirana H, Santosa P, Rinastiti M. Perawatan ekstrusi dan luksasi gigi molar satu mandibula dengan restorasi endocrown fiber reinforced composite Extrusion and luxation treatment of mandibular first molar with endocrown fiber-reinforced composite restoration. J Kedokt Gigi Univ Padjadjaran. 2022;33(3):28. doi:10.24198/jkg.v33i3.33250

21.	Ronca S. Polyethylene. Elsevier Ltd; 2017. doi:10.1016/B978-0-323-35824-8.00010-4

22.	Peijs T, Kirschbaum R, Jan P. Advanced Industrial and Engineering Polymer Research Chapter 5 : A critical review of carbon fi ber and related products from an industrial perspective. Adv Ind Eng Polym Res. 2022;5(2):90-106. doi:10.1016/j.aiepr.2022.03.008

23.	Marques S, Spyrides M, Prado M, Araujo JR De, Simão RA. Effects of plasma on polyethylene fiber surface for prosthodontic application. 2015;(February 2016). doi:10.1590/1678-775720150260

24.	Hussain M, Naqvi RA, Abbas N, Khan SM. ( UHMWPE ) as a Promising Polymer Material for Biomedical Applications : A Concise Review. Polymers (Basel). 2020;12(323):1-28.

25.	Li W, Hu H. Study on Preparation of Ultrahigh Molecular Weight Polyethylene Fibers. Adv Comput Sci Res. 2018;78(Iwmecs):15-18.

26.	Zamora-Mendoza L, Gushque F, Yanez S, et al. Plant Fibers as Composite Reinforcements for Biomedical Applications. Bioengineering. 2023;10(7):1-23. doi:10.3390/bioengineering10070804

27.	Murdiyanto D, Pratiwi SG. Pengaruh Penambahan Serat Kapas (Gossypium sp.) Terhadap Kekuatan Fleksural Resin Komposit Flowable. JIKG (Jurnal Ilmu Kedokt Gigi). 2019;2(1):1-5. doi:10.23917/jikg.v2i1.4863

28.	Faizah A, Pratiwi FI. Pengaruh Jumlah Aplikasi Silane Terhadap Kekerasan Fiber Reinforced Composite. JIKG (Jurnal Ilmu Kedokt Gigi). 2022;5(2):2-7.

29.	Chiayi Shen  and HRRAKJ. Phillips’ Science of Dental Material. 12th ed. Elsevier Health Sciences; 2016.

30.	Agunsoye JO, Aigbodion VS. Bagasse filled recycled polyethylene bio-composites: Morphological and mechanical properties study. Results Phys. 2019;3:187-194. doi:10.1016/j.rinp.2013.09.003

31.	Kumar N, Fareed MA, Zafar MS, Ghani F, Khurshid Z. Influence of various specimen storage strategies on dental resin-based composite properties. Mater Technol. 2021;36(1):54-62. doi:10.1080/10667857.2020.1728058

32.	Rezvani MB, Atai M, Hamze F. Effect of fiber diameter on flexural properties of fiber-reinforced composites. Indian J Dent Res. 2015;24(2):237-241. doi:10.4103/0970-9290.116696